## Slide 1: Host/guest complexes of coordination cages: catalysis and photophysical properties Michael Ward, University of Warwick, UK

## Slide 2: Ligands like these….

## Slide 3
M6L9 trigonal prism
M4L6 tetrahedron
M8L12 cube
M8L12 cuneane
M12L18 truncated
tetrahedron
M16L24 tetra-capped truncated tetrahedron
… give cages like these with M2+ ions

## Slide 4
Octanuclear cubic cage is a stable, nicely-sized host
V = 407 Å3
Optimal guest size, 224 Å3
Window diameter ≈ 4Å
Anions located around surface

## Slide 5
Water-soluble analogue for better guest binding
MeCN soluble Co8L12 host cage
Water soluble Co8L12 host cage

## Slide 6
Hydrophobic effect ensures strong binding of guests in water
Binding constants 103 – 106 M-1 in water depending on hydrophobic surface area / goodness of fit
1:1 binding from many luminescence / NMR titrations and crystal structures

## Slide 7
Guests H-bond to cage interior surface

## Slide 8
Windows on surface provide anion binding pockets
[BF4]–
Cl–
[NO3]–
I–

## Slide 9
Binding of guests related to hydrophobic surface area
C5
C13
• Perfectly linear increase in ∆G with hydrophobic surface area (5 kJ/mol per CH2 group)
• Matches results from protein folding (Alan Fersht)
• Decrease in ∆G above ‘Rebek limit’ (55% of cavity volume) as guests get too large
• Best guest (C11 ketone) has
K = 1.2 x 106 M-1 in water
JACS, 2014, 126, 8475

## Slide 10
‘High energy’ water in the cage cavity
• Cluster of 10 water molecules in cavity
• Average number of H-bonds = 3 per water (cf. 3.7 in solution)
• Consistent with ‘high energy water’ picture associated with cucurbiturils
(Biederman, Uzunova, Scherman, Nau, De Simone – JACS 2012, 134, 15318)

## Slide 11
Van’t Hoff experiments
 | ∆H | T∆S (298 K)
C7-one | –22 kJ/mol | –7
C8-one | –27 | –6
C9-one | –32 | –6
C8-one
• For each guest, ∆H >> T∆S – consistent with liberation of high-energy water
• For each incremental addition of CH2 group:
∆∆H = ca. 5 kJ/mol
T∆∆S = ca. 0 kJ/mol
Hydrophobic effect associated with each additional CH2 is predominantly ∆H: liberation of ‘high-energy’ water
Chem. Eur. J. 2018, 24, 1554

## Slide 12
B
Catalysis in the cage cavity
Expulsion of anionic product from cage provides basis for catalytic turnover

## Slide 13
Reaction can easily be followed by 1H NMR:
0 s
46950 s
≈ 13h

## Slide 14
0 s
31 s
97 s
163 s
295 s
229 s
361 s
Clear acceleration in presence of cage
≈ 6 min
HO–

## Slide 15
Background
With cage
Chart: Time / s
| 0.0 | 30.0 | 60.0 | 90.0 | 120.0 | 180.0 | 240.0 | 361.0 | 427.0 | 571.0 | 704.0 | 837.0 | 970.0
ph9.8 | 0 | 0.000474 | 0.000697 | 0.000796 | 0.000823 | 0.00084053 | 0.000845 | 0.000845 | 0.000845 | 0.000845 | 0.000845 | 0.000845 | 0.000845
 | 0 | 2.9894e-06 | 4.9824e-06 | 7.9718e-06 | 1.116e-05 | 3.236e-05 | 2.9419e-05 | 5.581e-05 | 6.2741e-05 | 9.9356e-05 | 9.6869e-05 | 0.00016223 | 0.00014468 | 0.00018594 | 0.00021662 | 0.00024704 | 0.00030089
kcat / kuncat = 4500
at pH 10
Maximum acceleration 2 x 105 at pH ≈ 8

## Slide 16
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
-OH
16+ charge on cage attracts –OH ions:
very high local concentration of –OH ions surrounding guest even at modest pH
-OH
Cage catalysis: co-location of reaction partners

## Slide 17
Cage catalysis – control experiments
Chart: pD
| 13.8 | 13.27712125471966 | 12.8 | 12.27712125471966 | 10.2
 | -1.4689 | -1.9859 | -2.4572 | -3.0229 | -5.0655
 | -1.4975 | -1.4176 | -1.3987 | -1.3855 | -1.4453
 | -1.4289 | -1.4289
 | -8.1856 | -8.1856

## Slide 18
1. Cycloundecanone displaces substrate: reaction now at uncatalysed rate
Cage catalysis – essential control experiments
-OH
-OH
-OH
-OH
-OH
-OH
Cl-
Cl-
Cl-
Cl-
Cl-
Cl-
Cl-
Cl-
2. XS Chloride ions bind more strongly to cage surface and displace hydroxides:
reaction now at uncatalysed rate

## Slide 19
• Two orthogonal interactions: hydrophobic cavity binds guest; cationic surface binds anions
• Multiple turnovers because anionic product is released (hydrophilic)
Nat. Chem. 2016, 8, 231

## Slide 20
X–
X–
X–
X–
General catalyst for bimolecular reactions?
Reactive neutral substrate, binds principally through hydrophobic effect
Anionic reaction partner surrounds substrate giving high local concentration
Two components can be varied independently of one another

## Slide 21
Changing the anion… onset of autocatalysis
Addition of Cl– not only inhibits reaction, it also changes its nature…
0 Cl–
16 mM Cl–
24 mM Cl–
32 mM Cl–
40 mM Cl–
48 mM Cl–
Sigmoidal profile indicates autocatalysis

## Slide 22
A B
Bcat
Initially slow as no catalyst present
Catalysis increases as B accumulates
Reactions slows as starting material consumed
Rebek and co-workers, PNAS 2010, 107, 541

## Slide 23
2-cyanophenolate (product) acts as base to deprotonate benzisoxazole
• Cl– displaces HO– from cage surface and shuts down Kemp elimination
• As 2-cyanophenolate forms it displaces Cl– from cage surface and acts as a base to catalyse its own formation
‘Soft’ anion, easily desolvated, high affinity for hydrophobic but cationic cage surface
phenolate > Cl– > HO–
JACS 2018, 140, 2821

## Slide 24
Dichlorvos – toxic organophosphate insecticide – destroyed by hydroxide
Binds weakly in cage cavity
K = 16 M-1 in water
What about other substrates in the cavity?

## Slide 25
Catalysed hydroysis: pD 7.5, 298K, observed by 31P NMR
SM
Prod
kcat / kuncat ≈ 1000
no cage
1 mM cage
Other phosphotriesters behave similarly with 103-fold acceleration of hydrolysis
unpublished

## Slide 26
One control experiment too far!
Blocking cavity with strongly binding cycloundecanone makes no difference to rate of disappearance of dichlorvos!
Conclusion: catalysed hydrolysis on cage exterior surface

## Slide 27
More control experiments!
(i) Use substrate that does not fit inside cavity at all
Chart: Time (s)
0.6 mM catalyst
‘Para-oxon’: another insecticide
No catalyst
0.12 mM catalyst

## Slide 28
(ii) Use a smaller cage with no significant cavity
Smaller M4L6 cage with cavity that only binds [BF4]– acts as comparably good catalyst for phospho-ester hydrolysis!
Crystal structure shows both starting material and 4-nitrophenolate product in contact with cage exterior surface

## Slide 30
Exterior surface is hydrophobic too (and has larger area)
Crystallographic evidence for interactions of other ‘guests’ with cage exterior surface
[BPh4]–
py–S–S–py

## Slide 31
Surface that is both hydrophobic and cationic
Contact of hydrophobic surfaces on cage exterior
HO–
HO–
HO–
accumulation of anions driven by ion-pairing
Same proximity of reactants – but not dependent on good match for cavity
“In this work, the authors illustrate a (sort of) novel property of self-assembled cage-based catalysis, in that solvolysis can be catalyzed at the exterior surface of highly cationic cages, rather than in the cavity. The conclusion is pretty obvious, really, and the kind of thing we will look back at in 10 years and say "well, of course that happens". Surface scientists and physical organic chemists would also probably say that this is obvious. However, I agree with the authors - this type of mechanism is definitely not considered when catalysis applications of cage hosts are studied.”
Chem. Eur. J., in press

## Slide 32
Another external-surface catalysed reaction
Indane-1,3-dione
Colourless
pKa ≈ 7
‘Bindone’ (purple) via aldol condensation
Guests inside cavity…
… and interacting with anion site on exterior surface (enolate anion??)

## Slide 33
Weak acid (pH ≈ 4) – no detectable aldol reaction in absence of cage
Catalysed reaction very slow (few % conversion after 12h): but happening!
Competing cavity-blocker makes little difference to rate profile
Co-location of neutral indane-dione and enolate anion around cage surface??
Stabilisation of enolate anions: valuable / general catalytic utility?

## Slide 34
Cages can act as assembly of multiple fluorophores surrounding single guest
K = 106 M-1
Sensitised pyrene-based emission by energy-transfer from naphthalene units

## Slide 35
K = 104 M-1
hn
e–
Transient signature of [TCNB]•–
Decays with 160 ps lifetime
Chem. Commun., 2017, 53, 408
Photoinduced electron transfer to TCNB guest

## Slide 36
Photo-redox catalysis on cavity–bound guests??
Photo-redox catalysis well-established using 1-electron PET agents such as [Ru(bipy)3]2+, [Os(bipy)3]2+ and Ir(III) complexes
Excited states are one- electron transfer agents which trigger reactions in oxidised or reduced substrates
Relies on collision in solution during lifetime of excited state

## Slide 37
Can we incorporate multiple metal complex chromophores as vertices of cage?
• Surround bound guest with multiple photocatalytic centres
• Guest / photocatalyst units held in close proximity
• Plenty of time for PET to occur as long excited-state lifetimes
8 M(II) ions + 12 ligands
(M = Ru, Os)
X
Self-assembly requires labile components!

## Slide 38
Two-step assembly based on kinetically inert components
• Initial preparation of kinetically inert [ML3]2+ (M = Ru / Os) building block
• Assembly with labile ion [Cd(II) / Zn(II)] to complete mixed-metal cube
• Inert / labile ions strictly alternate around periphery of Ru4Cd4 structure
• Can get four photosensitisers built into one cage assembly
Chem. Comm., 2014, 50, 6330
Dalton Trans., 2015, 44, 17939

## Slide 39
[Os(py-pz)3]2+ vertices are excellent photo-electron donors
3MLCT energy ≈ 16000 cm-1
t (solution) ≈ 100 ns
Os(II)/Os(III), +0.43 V vs Fc
• Better photo-electron donor than [Ru(bipy)3]2+
• Capable of effecting PET to range of bound electron-accepting guests
Dalton Trans., 2015, 44, 17939

## Slide 40
Transient absorption spectra show charge-separated Os3+ / (guest)•– states following cage-to-guest PET
Quenching of Os4Zn4 cage by NQ

## Slide 41
Kinetic measurements show formation (20 ps) and decay (200 ps) of charge-separated state
Addition of competing guest removes short transients confirming that guest is bound in cavity
Inorg. Chem., 2019, 58, 2386

## Slide 42
Synthesis / host guest chemistry / photophysics / catalysis
Will Cullen
Chris Taylor
Alex Metherell
Jerico Piper
Ashley Wragg
Jennifer Train
Stephen Argent
Cristina Mozaceanu
Funding:
EPSRC
Leverhulme Trust
EU (‘NOAH’ ITN)
Collaborators: Chris Hunter
Nick Williams
Julia Weinstein

## Slide 43
Thank you
Questions?